SECTION 07 21 53 – REFLECTIVE INSULATION

GENERAL

SUBMITTALS

Action Submittals:

Product Data: Manufacturer’s descriptive data and product attributes for insulation.

Informational Submittals:

Certificate of Compliance: Certification that installed products meet specified fire hazard requirements.

QUALITY ASSURANCE

Installer Qualifications: Firm specializing in work of this Section with minimum [2] [__] years’ experience.

PRODUCTS

MANUFACTURERS

Contract Documents are based on products by Fi-Foil Company, Inc., www.fi-foil.com

Substitutions: [Refer to Division 01.] [Not permitted.]

MATERIALS

Reflective Insulation:

Source: VR Plus Shield™.

Thermal Performance: Comply with ASTM C1224.

Description: Multi-layer reflective wall insulation.

Outer Layer:  White kraft paper coated with polyethylene.

Middle Layer:  Natural Kraft paper aluminum foil laminate.

Inner Layer:  Aluminum foil.

Layers separate with internal expanders, creating reflective air space when installed.

Type: [Perforated.] [Non-perforated (solid).]

Tabs: [Staple tabs.] [Tape tabs.]

Flammability: Flame Spread [<25] [<45] and Smoke Developed <450, tested to ASTM E84 in accordance with E2599.

Water Vapor Permeance: [8.0 perms] [0.0 perms], tested to ASTM E96.

Delamination & Corrosion: None, tested to ASTM C1258.

Fungi Resistance: Pass, tested to ASTM C1338.

Thermal Emittance: ≤0.1, tested to ASTM C1371.

**** OR ****

Reflective Insulation:

Source: M-Shield®.

Thermal Performance: Comply with ASTM C1224.

Description: Single-layer paperless reflective wall insulation.

Inside Layer: Aluminum foil.

Outside Layer: Synthetic polymers with zero cellulose.

Layers separate with internal expanders, creating reflective air space when installed.

Flammability – Class A: Flame Spread <25 and Smoke Developed <450, tested to ASTM E84 in accordance with E2599.

Water Vapor Permeance: 7.5 perms, tested to ASTM E96.

Delamination & Corrosion: None, tested to ASTM C1258.

Fungi Resistance: Pass, tested to ASTM C1338.

Thermal Emittance: ≤0.1, tested to ASM C1371.

**** OR ****

Reflective Insulation:

Source: AA2 Shield™.

Thermal Performance: Comply with ASTM C1224.

Description: Single-layer reflective wall insulation.

Inside Layer: Aluminum foil.

Outside Layer: Kraft paper coated with polyethylene.

Layers separate with internal expanders, creating reflective air space when installed.

Type: [Perforated.] [Non-perforated (solid).]

Tabs: [Staple tabs.] [Tape tabs.]

Flammability: Flame Spread <75 and Smoke Developed <450, tested to ASTM E84 in accordance with E2599.

Water Vapor Permeance: [6.5 perms] [<1.0 perms], tested to ASTM E96.

Delamination & Corrosion: None, tested to ASTM C1258.

Fungi Resistance: Pass, tested to ASTM C1338.

Thermal Emittance: ≤0.1, tested to ASTM C1371.

**** OR ****

Reflective Insulation:

Source: RBI Shield™.

Thermal Performance: Comply with ASTM C1224.

Description: Reflective bubble insulation, [polyethylene.] [reflective.]

Type: Double bubble.

Flammability: Flame Spread 0 and Smoke Developed <50, tested to ASTM E84.

Water Vapor Permeance: ≤0.1, tested to ASTM E96

Temp & Humidity Resistance: None, tested to ASTM C1258.

Fungi Resistance: Pass, tested to ASTM C1338.

Thermal Emittance: 0.06, tested to ASTM C1371.

Hot Surface Performance: <250 degrees Fahrenheit; tested to ASTM C411.

UV Exposure; 105 percent retention after 2,000 hours; tested to ASTM G155.

ACCESSORIES

Tape: [1170 Aluminum Foil Tape by 3M or equivalent.] [FS-K7751 FSK Insulation Facing Tape by Echo Tape or equivalent.]

**** OR ****

Tape: [PE-M4535 Silver] [PE-M4535 White] by Echo Tape or equivalent.

Mechanical Fasteners: Provided by insulation manufacturer; type best suited to application.

EXECUTION

INSTALLATION

Install insulation in accordance with manufacturer’s instruction.

- END OF SECTION