Fi-Foil Company, Inc.	November 2025

PO Box 800

Auburndale, Florida 33823

Toll Free	800-448-3401

Phone	863-965-1846

Fax	863-967-0137

Website	www.fifoil.com

E-mail	marketing@fifoil.com

Product Guide Specification

Specifier Notes: This product guide specification is written according to the Construction Specifications Institute (CSI) 3-Part Format, including MasterFormat, SectionFormat, and PageFormat, as described in The CSI Construction Specifications Practice Guide.

This section must be carefully reviewed and edited by the Architect to meet the requirements of the project and local building code.  Coordinate this section with other specification sections and the Drawings.  Delete all “Specifier Notes” after editing this section.

Section numbers and titles are based on MasterFormat 2020 Update.

07 21 54

RADIANT BARRIER INSULATION

Specifier Notes:  This section covers FI-FOIL® Silver Shield™ radiant barrier insulation intended for use in roof cavities for attic radiant barrier applications and walls facing attic spaces.  Consult Fi-Foil Company for assistance in editing this section for the specific application.

GENERAL

SECTION INCLUDES

Radiant barrier insulation.

RELATED REQUIREMENTS

Specifier Notes:  Edit the following list of related sections as necessary.  Limit the list to sections with specific information that the reader might expect to find in this section, but is specified elsewhere.

Section 06 11 00 – Wood Framing.

Section 07 26 00 – Vapor Retarders.

Section 07 27 00 – Air Barriers.

Section 09 22 13 – Metal Furring.

REFERENCE STANDARDS

Specifier Notes: List reference standards used elsewhere in this section, complete with designations and titles.

ASTM C1136 – Standard Specification for Flexible, Low Permeance Vapor Retarders for Thermal Insulation.

ASTM C1224 – Standard Specification for Reflective Insulation for Building Applications.

ASTM C1313 – Standard Specification for Sheet Radiant Barriers for Building Construction Applications.

ASTM C1338 – Standard Test Method for Determining Fungi Resistance of Insulation Materials and Facings.

ASTM C1371 – Standard Test Method for Determination of Emittance of Materials Near Room Temperature Using Portable Emissometers.

ASTM C1743 – Standard Practice for Installation and Use of Radiant Barrier Systems (RBS) in Residential Building Construction.

ASTM C1744 – Standard Practice for Installation and Use of Radiant Barrier Systems (RBS) in Commercial/Industrial Building Construction.

ASTM D2261 – Standard Test Method for Tearing Strength of Fabrics by the Tongue (Single Rip) Procedure (Constant-Rate-of-Extension Tensile Testing Machine.

ASTM D3310 – Standard Test Method for Determining Corrosivity of Adhesive Materials.

ASTM E84 – Standard Test Method for Surface Burning Characteristics of Building Materials.

ASTM E96 – Standard Test Methods for Water Vapor Transmission of Materials.

ASTM STP 1116 – Insulation Materials: Testing and Applications.

SUBMITTALS

Specifier Notes: Edit submittal requirements as necessary.  Delete submittals not required.

Comply with Section 01 33 00 – Submittal Procedures.

Product Data: Submit manufacturer’s product data, including installation instructions.

Samples: Submit manufacturer’s sample of radiant barrier insulation, minimum 6 inches square.

Manufacturer’s Certification: Submit manufacturer’s certification that materials comply with specified requirements and are suitable for intended application.

Sustainable Design Submittals: Submit manufacturer’s sustainable design submittals.

Recycled Content: Certify percentages of pre-consumer and post-consumer recycled content.

Warranty Documentation: Submit manufacturer’s standard warranty.

QUALITY ASSURANCE

Manufacturer’s Qualifications: Manufacturer regularly engaged, for a minimum of 10 years, in the manufacturing of radiant barrier insulation of similar type to that specified.

DELIVERY, STORAGE, AND HANDLING

Delivery Requirements: Deliver materials to site in manufacturer’s original, unopened containers and packaging, with labels clearly identifying product name and manufacturer.

Storage and Handling Requirements:

Store and handle materials in accordance with manufacturer’s instructions.

Keep materials in manufacturer’s original, unopened containers and packaging until installation.

Store materials in clean, dry area indoors.

Protect materials during storage, handling, and installation to prevent damage.

PRODUCTS

MANUFACTURERS

Manufacturer: Fi-Foil Company, Inc., PO Box 800, Auburndale, Florida 33823.  Toll Free 800-448-3401.  Phone 863-965-1846.  Fax 863-967-0137.  Website www.fifoil.com.  E-mail marketing@fifoil.com.

Specifier Notes:  Specify if substitutions will be permitted.

Substitutions: [Not permitted] [In accordance with Division 1].

RADIANT BARRIER INSULATION

Radiant Barrier Insulation:  Fi-Foil® Silver Shield™.

Description:

Multiple layers of low emittance (low-e) materials designed to significantly reduce radiant  heat transfer.

Inside Layer: Metalized polymer.

Outside Layer: Reinforced aluminum foil kraft paper bonded with fire retardant adhesive.

Reflective Air Space: Layers expand when installed to form reflective air space to provide thermal performance and protect low-e surface from performance-reducing effects of dust accumulation.

Tabs: Reinforced staple tabs.

Compliance and Approvals:

Compliance: Meets ASTM C1313.

State of California Bureau of Furnishings and Thermal Insulation License #T390, updated 9/08/2025.

Third Party Verification:

Recycle Content of Fi-Foil® Products, verified by R & D Services, Inc. See www.fifoil.com for latest version of Report.

Testing:

- Water Vapor Permeance, ASTM E96: 5 perms.

Flammability, ASTM E 84:

Flame Spread: Less than 25.

Smoke Developed: Less than 450.

Interior Wall and Ceiling Finish Classification: Class A.

Thermal Emittance, ASTM C1371:

First Layer, MET PVC Metal Side: 0.04.

Second Layer, Foil Laminate: 0.03.

R-Values for Reflective Air Space, ASTM STP 1116:

Heat Flow Horizontal (single low-e surface): 1.7.

Corrosivity, ASTM D3310: Pass.

Adhesive Performance, ASTM C1224:

Bleeding: None.

Delamination: None.

Pliability: No signs of cracking or delamination.

Tongue Tear Test, ASTM D2261:

Machine Direction (MD): 1.77.

Cross-Machine Direction (CD): 2.32.

Mold and Mildew Resistance, ASTM C1338: Pass.

ACCESSORIES

Facing Tape: 3M™ Venture Tape™ FSK Facing Tape or equivalent.

Description: Foil, scrim and kraft laminate backing for use on fibrous and sheet metal ducts.

Facing Tape: 3M™ Venture Tape™ Aluminum Foil Tape or equivalent.

Description: Multi-purpose foil tape for a variety of applications.

EXECUTION

EXAMINATION

Examine areas to receive radiant barrier insulation.

Notify Architect of conditions that would adversely affect installation.

Do not begin installation until unacceptable conditions are corrected.

INSTALLATION

Install radiant barrier insulation in accordance with manufacturer's instructions and ASTM C 1158.

Install radiant barrier insulation at locations indicated on the Drawings.

Splice radiant barrier insulation in accordance with manufacturer's instructions to avoid gaps.

Tape seams if gaps appear where splice has been butted.

Tape tears in radiant barrier insulation.

Replace damaged radiant barrier insulation as directed by Architect.

PROTECTION

Protect installed radiant barrier insulation from damage during construction.

END OF SECTION