SECTION 07 27 00 – AIR BARRIERS

GENERAL

SUBMITTALS

Action Submittals:

Product Data: Manufacturer’s descriptive data and product attributes for air barrier.

Informational Submittals:

Certificate of Compliance: Certification that installed products meet specified fire hazard requirements.

QUALITY ASSURANCE

Installer Qualifications: Firm specializing in work of this Section with minimum [2] [__] years’ experience.

Provide air barrier and foil tape from single manufacturer.

PRODUCTS

MANUFACTURERS

Contract Documents are based on products by Fi-Foil Company, Inc., www.fi-foil.com

Substitutions: [Refer to Division 01.] [Not permitted.]

MATERIALS

Air Barriers:

Source: SkyFlex™ (Solid).

Description: Two layers of aluminum deposited on layer of woven polyethylene.

Flammability, Class A: Flame Spread Less than 25 and Smoke Developed Less than 50, tested to ASTM E84.

Performance characteristics:

Air Permeability: Less than 0.02 liters per second per square meter at 75 Pa, tested to ASTM E2178.

Water Vapor Permeance: Less than 0.1 perm, tested to ASTM E96.

Emissivity: 0.05, tested to ASTM C1371.

ACCESSORIES

Aluminum Foil Tape: PE-M4535 Silver by Echo Tape or equivalent.

FSK Insulation Facing Tape: FS-7751 by Echo Tape or equivalent.

EXECUTION

INSTALLATION

Install insulation in accordance with manufacturer’s instructions.

END OF SECTION